OP901

AkroFlex Barrier EIF System Specification

This document contains Omega Products International’s specification for the AkroFlex Barrier Exterior Insulation and Finish System (EIFS).  The AkroFlex Barrier System is a class PB barrier EIF system that is comprised of a water-resistive/air barrier (optional), adhesively attached foam insulation, base coat with embedded mesh, primer (optional), and a finish coat.

The specification is intended to be tailored by the design professional to suit the project requirements and follows the Construction Specification Institute’s (CSI) MasterFormat (2016 Ed.) and SectionFormat (2009 Ed.).  are locations where information needs to be added or deleted depending upon project needs.  These locations are indicated using the following formatting:

[Notes]	Notes that provide instructions or guidance.  These should be deleted when no longer needed.

[Options]	Possible options for the system.  Choose one, or in some cases, more than one can be selected, and delete the remaining options.  Delete the brackets and un-bold the selected option(s).

<Text>	Locations where text needs to be inserted.

This specification should be used along with other AkroFlex Barrier documentation including the standard system details (APB), system data sheet, Intertek CCRR report, and individual product data sheets.   Please visit www.omega-products.com to obtain these documents and for additional information on the AkroFlex EIF Systems.

Mar 2023

SECTION 07 24 13 – AKROFLEX BARRIER EIFS

PART 1- GENERAL

- SUMMARY

- Section Includes:  Work includes all labor, materials, and equipment necessary to install all aspects of the AkroFlex Barrier Exterior Insulation and Finish System (EIFS).

- Related Sections [Delete unneeded sections]

    - 03 30 00 – Cast-in-Place Concrete

    - 04 20 00 – Unit Masonry

    - 05 40 00 – Light gauge cold-formed steel framing

    - 06 11 00 – Wood Framed Construction

    - 06 16 00 – Sheathing

    - 07 90 00 – Joint Sealers

    - 09 29 00 – Gypsum Board

    - 07 27 00 – Air Barriers

    - REFERENCES [Delete unneeded references]

  - AATCC Test Method 127 – Water Resistance

  - ASTM B117 – Salt Spray Testing

  - ASTM C79/C1396 – Gypsum Sheathing Specification

  - ASTM C1325 – Cement Board Sheathing

  - ASTM C150 – Portland Cement Specification

  - ASTM C297 – Flatwise Tensile Strength Testing

  - ASTM C920 – Elastomeric Joint Sealants

  - ASTM C1397 –  Application of Class PB Exterior Insulation and Finish Systems

  - ASTM D968 – Abrasion Resistance Testing

  - ASTM D1784 – Specifications for Rigid PVC and Chlorinated Poly Vinyl Chloride (CPVC) compounds

  - ASTM D1970 – Fastener Sealability

  - ASTM D2247 – Water Resistance Testing

  - ASTM D3273 – Resistance to Growth of Mold on the Surface of Interior Coatings

  - ASTM E72 – Conducting Strength Tests of Panels for Building Construction

  - ASTM E84 – Flame Spread and Smoke Density Testing

  - ASTM E96 - Water Vapor Transmission of Materials

  - ASTM E108 (Modified) – Modified Fire Testing

  - ASTM E283 – Air Leakage

  - ASTM E330 – Negative and Positive Load Testing

  - ASTM E331 – Water Penetration Testing

  - ASTM E695 – Impact Resistance Testing

  - ASTM E1233 – Structural Performance by Cyclic Air Pressure Differential

  - ASTM E2178 – Air Permeance

  - ASTM E2357 – Air Barrier Assembly

  - ASTM E2485 – Freeze/Thaw Resistance of EIFS and WRB Coatings

  - ASTM G155 – Accelerated Weathering

  - NFPA Method 268 – Radiant Heat Resistance Test

  - NFPA Method 285 – Fire Propagation Evaluation for Exterior Walls

  - UBC 26-4 (Formerly UBC 17-6) – Multi-Story Fire Testing

  - ICC-ES AC212 – Acceptance Criteria for Water-Resistive Coatings

  - ICC-ES AC219 – Acceptance Criteria for Exterior Insulation and Finish Systems

  - Intertek CCRR-0466

  - Intertek CCRR-0465

  - Omega AkroFlex Barrier Systems Details (APB)

  - system description

  - General:  The AkroFlex Barrier System is a class PB barrier EIF system that is comprised of a water-resistive barrier/air coating (optional), adhesively attached foam insulation, base coat with embedded mesh, primer (optional), and a finish coat.

  - Application Methods:  The AkroFlex system is applied directly to a structure at the construction site or may be applied to prefabricated panels.

  - Design Requirements and Limitations: [This section is primarily for reference and may be deleted.]

    - Substrates:  Compatible substrates with the AkroFlex Barrier System

      - Sound, unpainted concrete, portland cement plaster, brick, or masonry.

      - Exterior Grade Gypsum sheathing conforming to ASTM C79 or C1396.

      - Exterior grade glass mat gypsum sheathing conforming to ASTM C1177.

      - Cement board sheathing complying to ASTM C1325.

      - Exterior or Exposure 1 rated plywood complying with U.S. DOC PS-1.

      - Exposure 1 OSB board complying with U.S. DOC PS-2.

    - Inclined Surfaces:  Slope a minimum of 6:12.  Do not use in horizontal applications or in locations where water may collect on the surface.  The length of inclined surfaces shall not exceed 12 inches (305 mm).

    - Deflection of the substrate system shall not exceed L/240.

    - Expansion Joints:  Joints must be installed as specified by the engineer, architect, designer, or builder, in that order.  At a minimum, the following locations should have expansion joints:

      - Where expansion joints occur in the substrate system.

      - Where building expansion joints occur.

      - Where prefabricated panels abut one another.

      - At floor lines in wood framed construction.

      - Where the AkroFlex System abuts dissimilar materials.

      - Where there is a change in substrates.

      - Where structural movement is anticipated.

    - Terminations

      - A minimum gap of ¾-inch (19 mm) shall be maintained at all EIFS to EIFS terminations.  Final design will depend on structural and sealant requirements.

      - A minimum gap of ½-inch (13 mm) shall be maintained at all EIFS to dissimilar materials.  Final design will depend on structural and sealant requirements.

      - Terminate insulation board a minimum 8 inches (203 mm) above finish grade and 6 inches (152 mm) above paved surfaces/hardscape.

      - Sealants used in conjunction with this system shall comply with the Intertek CCRR-0466 report.  The backer rod used with this system shall be the closed cell type.

    - Color Section: It is not recommended to select dark finish coat colors.

  - Performance [This section is primarily for reference and may be deleted.]

    - Water-Resistive/Air Barrier [Delete this table if the optional water-resistive/air barrier is not used.]

| Test | Test Method | Criteria | Results |
| --- | --- | --- | --- |
| Tensile Bonding | ASTM C297 | Strength >15 psi (103 kPa) | Passed |
| Freeze-Thaw | ASTM E2485 Method B | No deleterious effects after 10 cycles | Passed |
| Water Resistance | ASTM D2247 | No deleterious effects from 14 days of exposure to water | Passed |
| Water-vapor Transmission | ASTM E96 | Vapor permeable | Passed: 1.58 g/hm2 |
| Structural & Water: - Transverse Load - Racking - Restrained Environmental Conditioning - Water Penetration | AC212: - ASTM E1233 - ASTM E72 - AC212 - ASTM E331 | No visible cracking after structural, racking, environmental conditioning; No visible water penetration at sheathing joints after 15 minutes at 2.86 psf (137 Pa) | Passed: No cracking; 175 minutes at 6.24 psf (299 Pa) |
| Weathering: - UV Resistance - Accelerated Aging - Hydrostatic Pressure | AC212: - AC212 - AC212 - AATCC Test Method 127-1985 | No cracking or bond failure; No water penetration of backside of sample | Passed |
| Surface Burning | ASTM E84 | Flame Spread <25 Smoke Index <450 | Flame Spread: 10 Smoke Index: 0 |
| Air Permeance | ASTM E 2178 | < 0.20 L/(s·m²) at 75 Pa [0.003 ft3/min·ft2 @ 1.56psf ] | Passed: .007 L/(s·m²) |
| Air Barrier Assembly | ASTM E 2357 | Not greater than 0.20 L/(s·m²) [0.003 ft3/min·ft2] tested in both directions | Passed: .009 L/(s·m²) |
| Air Leakage | ASTM E283 | < 0.20 L/(s·m²) at 75 Pa [0.003 ft3/min·ft2 @ 1.56psf ] | Passed: .007 L/(s·m²) |
| Water Resistance | AATCC 127-03 | No water penetration | Passed |
| Fastener Sealability | ASTM D 1970 | No water penetration at nail penetration under 127mm (5 in) head or water after 3 days at 4ºC (40ºF) | Passed |

    - EIF System

| Test | Test Method | Criteria | Results |
| --- | --- | --- | --- |
| Accelerated Weathering | ASTM G155 | No deleterious effects after 2000 hours | Passed: 5000 hours |
| Freeze-Thaw | ASTM E2485 Method A (formerly EIMA 101.01) | No deleterious effects after 60 cycles | Passed: 90 cycles |
| Freeze-Thaw | ASTM E2485 Method B | No deleterious effects after 10 cycles | Passed |
| Water Resistance | ASTM D2247 | No deleterious effects after 14 days | Passed: 42 days |
| Mildew Resistance | ASTM D3273 | No growth during 28-day exposure | Passed |
| Salt Spray Resistance | ASTM B117 | No deleterious effects after 300 hours | Passed: 1000 hours |
| Water Penetration | ASTM E331 / AC 219 | No water penetration beyond the inner-most plane of the wall after 15 minutes at 137 Pa (2.86 psf) | Passed 15 minutes at 137 Pa (2.86 psf) |
| Water-vapor Transmission | ASTM E96 | Vapor permeable | 10 to 31 perms |
| Abrasion Resistance | ASTM D968 | No deleterious effects after 500 liters (528 quarts) | Passed: 1000 liters (1056 quarts) |
| Tensile Bonding | ASTM C297 | Strength >15 psi (103 kPa) | Passed |
| Full Scale Diversified Fire Test | ASTM E108 Mod. | No significant contribution to vertical or horizontal flame spread | Passed |
| Full Scale Multi-Story Fire Test | UBC Std. 26-4 (formerly 17-6) | Resist spread of flame | Passed |
| Intermediate Multi-Story Fire Test | NFPA 285 (UBC 26-9) | Resist spread of flame | Passed |
| Surface Burning | ASTM E84 | Flame Spread < 25 Smoke Index < 450 | Flame Spread: 20 Smoke Index: 5 |
| Ignitability | NFPA 268 | No ignition at 12.5 kw/m2 at 20 minutes | Passed |

- submittals

  - Product Data:  All product data sheets, evaluation reports, details, and warranty information that pertain to the project in accordance with Section 01 30 00 Submittal Procedures.

  - Samples:  Submitted upon request.

    - Samples of the finish coat shall be of an adequate size as required to represent each color and texture to be utilized on the project and produced using the same techniques and tools required to complete the project.

    - Retain approved samples at the construction site throughout the application process.

    - Quality Assurance

  - Qualifications:

    - Manufacturer:  System component materials shall be manufactured or approved by Omega Products International and shall be distributed by the same or its authorized dealers.

  - Plastering Contractor:

    - Shall specialize in EIFS installation with documented experience.

    - Shall provide proof of current contractor's license and bond where required.

    - Shall show proof of current Approved Applicator Certificate issued by Omega Products International.

  - On-Site Mock-ups:  Produced upon request.

    - Prior to commencement of work, provide a mock-up for approval.

    - Mock-up suitable to represent the products to be installed for each color and texture constructed using the same tools and techniques to be utilized on the project.

    - Retain approved mock-up at job site throughout the application process.

      - Where acceptable to the architect, approved mock-ups may become part of the completed work if undisturbed at time of substantial completion.

      - DELIVERY, STORAGE, AND HANDLING

  - Delivery:  Deliver all materials to the construction site in their original, unopened packaging with labels intact.

  - Inspection:  Inspect the materials upon delivery to ensure that specified products have been received.  Report defects or discrepancies to the responsible party according to the construction documents; do not use reported material for application.

  - Storage:  Store all products per manufacturer's recommendations.  Generally, store materials in a cool, dry location; away from direct contact with the ground and/or concrete; out of direct sunlight; and protect from weather and other damage.

  - Project Conditions

  - Environmental Requirements:  Follow product data sheet's recommendations for environmental conditions and surface preparation.

    - Temperatures:  Before, during and following the application of the AkroFlex adhesive, base coat, and finish, the ambient and surface temperatures must remain above 40°F (4°C) for a minimum period of 24 hours.   Protect materials from uneven and excessive evaporation, especially during hot, dry, windy weather.   Protect from freezing for a period of not less than 24-hours after application has occurred.

    - Substrates:  Prior to installation, inspect the wall for surface contamination or other defects that may adversely affect the performance of the materials.  Do not apply AkroFlex EIFS to substrates whose temperature are less than 40°F (4°C), containing frost, ice, or residual moisture.

    - Inclement Weather:  Protect applied material from inclement weather until dry.

  - Existing Conditions:

    - Jobsite Resources:  Provide access to electrical outlets, potable water, and a suitable work area at the construction site throughout the application of the AkroFlex System.

    - Sequencing and Scheduling

  - Sequencing:  Coordinate the installation of the AkroFlex System with all other construction trades.

  - Staffing:  Provide sufficient manpower to ensure continuous operation, free of cold joints, scaffolding lines, variations in texture, etc.

  - Warranty

  - System Warranty:  Submit documentation on AkroFlex's standard system warranties.  At completion of work, provide written system warranty documentation.

  - Warranty Length: [Ten (10)] [Twelve (12)] [Thirteen (13)] [Fifteen (15)] [Eighteen (18)] years commencing at the time of substantial completion.  [See Omega Product's System Warranties for more information.  The warranty length depends upon the combination of products used in the system.]

  - Maintenance

  - The following materials shall be presented to the owner following the application of the AkroFlex System:

    - Color and texture information utilized on the project.

    - A maintenance program for finishes as required.  Refer to Omega's Technical Bulletin OP810 AkroFlex EIFS Maintenance Guide.

    - A maintenance program for sealants.  A minimum annual inspection should be conducted.  Refer to sealant manufacturer for additional information.

PART 2 - PRODUCTS

- Manufacturers

- Acceptable Manufacturer: Omega Products International.

- Compatibility

- Compatibility:  Provide adhesive, fasteners, insulation board, reinforcing meshes, base coats, finishes, sealants, and accessories that are compatible with one another and with substrates and approved for use by Omega Products International for the project.

- Water-Resistive air Barrier assembly [Delete if the optional water-resistive/air barrier is not used.]

- AkroGuard: An acrylic-based water-resistive barrier coating manufactured by Omega Products International.

- Joint/Transition Treatments [Delete the options not used.]

    - AkroFill: An acrylic-based water-resistive coating manufactured by Omega Products International.

    - AkroFlex Starter Mesh:  Are 4.2oz. alkali-resistant woven glass fiber fabrics specially designed to be used with AkroFill by Omega Products International.

    - AkroGuard Fabric: A reinforced non-woven polyester fabric designed to be used with AkroGuard by Omega Products International.

    - EIFS/Stucco Tape:  A self-adhered, rubberized asphalt membrane with a polyester top surface by Protecto Wrap.

- Adhesives

- [Choose one or more of the adhesive options and delete the remaining.]

- [ StyroGlue DryBond:  A factory-blended, polymer-modified cement-based material.]

- [StyroGlue:  A 100% polymer-based base coat and adhesive, which is field mixed in a 1:1 ratio by weight with portland cement complying with ASTM C150.]

- [StyroGlue Plus:  A 100% polymer-based, fiber-reinforced, water-resistant base coat and adhesive, which is field mixed in a 1:1 ratio by weight with portland cement complying with ASTM C150.]

- [StyroBond:  A non-cementitious, 100% acrylic adhesive designed to bond EPS foam to various approved substrates including wood-based sheathing.] [StyroBond shall not be used over AkroGuard or to bond EPS to EPS.]

- Insulation Board

- Expanded polystyrene board complying with ASTM C578, Type I, with a nominal density of 1 pound per cubic foot, a flame-spread rating of 25 or less, a smoke-developed rating not exceeding 450, a thickness of <insert thickness>, a maximum dimension of 2-foot (60 cm) x 4-foot (120 cm), and shall be produced by a manufacturer approved by Omega Products International.  [EPS board thickness shall be between 1 and 4-inches (25 and 102 mm), have a minimum thickness of ¾-inch (19 mm) after rasping, and shall conform to the applicable building codes.]

- Reinforcing Mesh

- AkroFlex Meshes:  Are alkali-resistant woven glass fiber fabrics specially designed to be used with AkroFlex EIF Systems.  [Different size and weight mesh may be required depending on the location and impact resistance needed.  Delete the options not used.]

    - Ultra Heavy Duty Mesh (20oz): For locations needing the highest impact resistance, such as ground floors and high traffic areas.

    - Heavy Duty Mesh (15oz): For locations needing high impact resistance, such as ground floors and other higher traffic areas.

    - Intermediate Mesh (11.5oz): For locations needing additional impact resistance, such as medium traffic areas.

    - Standard Mesh (4.2oz): For locations needing standard impact resistance, such as second stories or other low traffic areas where impact is unlikely.

    - Starter Mesh (4.2 oz.): For back wrapping and detail work.

- Base Coat

- [Choose one or more of the base coat options and delete the remaining.]

- [StyroGlue DryBond:  A factory-blended, polymer-modified cement-based material.]

- [StyroGlue:  A 100% polymer-based base coat and adhesive, which is field mixed in a 1:1 ratio by weight portland cement complying with ASTM C150.]

- [StyroGlue Plus:  A 100% polymer-based, fiber-reinforced, water-resistant base coat and adhesive, which is field mixed in a 1:1 ratio by weight with portland cement complying with ASTM C150.] [StyroGlue Plus is recommended for those areas where high moisture is expected such as sills or parapet applications.]

- [StyroGlue TF:  A 100% acrylic water-based, fibered, non-cementitious base coat manufactured to be flexible and crack-resistant.]

  - [Optional OmegaCure may be used to accelerate the hydration of the cementitious base coats.  Delete this section if not used.]

[OmegaCure: A non-corrosive liquid admixture for accelerating the hydration of cement base coats or adhesives.]

- Accessories

[Delete the accessories from this section as needed]

- Sealant:  Must be compatible with EIFS components and adjacent materials, be approved by Omega Products, and must meet ASTM C920 (Type S or M, minimum Grade NS, minimum Class 25, and Use O sealant).

- Flashing:  Flashing complying with local code, IBC Section 1405.4, or IRC Section R703.4, as applicable, must be provided.  Rigid flashings must be sloped towards the exterior, with an upturned leg on the interior side and at the ends, and must extend beyond the surface of the exterior wall.

- Fasteners:  Nails, staples, or screws used to rigidly secure associated accessories shall be corrosion-resistant and suitable for the substrate and/or framing.

- Trim:  Fabricated from high-impact PVC.

- Primer

- [Primer is optional, but is recommended.  The use of primer will increase the AkroFlex system warranty by 3 years.  Delete this section if primer will not be used on the project.]  AkroFlex Base Primer manufactured by Omega Products International.

- Finishes

- [Choose one or more of the following finishes and delete the remaining ones.  The use of AkroSil or AkroLastic will increase the AkroFlex system warranty by 2 years.]

- [AkroFlex <insert finish name>:  100% acrylic-based finish manufactured by Omega Products International.]

- [AkroSil <insert finish name>: Silicone-enhanced acrylic-based finishes manufactured by Omega Products International.]

- [AkroLastic <insert finish name>:  Elastomeric acrylic-based finishes manufactured by Omega Products International.]

- [AkroLastic ProPlus <insert finish name>:  Premium elastomeric acrylic-based finishes manufactured by Omega Products International.]

- Color and Texture:  Color and finish texture shall be as selected by the Architect.

- Mixes

- All material mixing instructions are contained in the appropriate Product Data Sheet written by Omega Products International.

PART 3 - EXECUTION

- EXAMINATION

- Substrates:

    - Acceptable substrates must be securely fastened per applicable building code requirements, the AkroFlex CCRR report, and/or sheathing manufacturer's recommendations.

    - Acceptable substrates and adjacent materials must be dry, clean, and sound.  Substrate surface must be flat, free of planar irregularities greater than 1/4-inch in 4 feet (6mm in 1.2m).

- Flashings:  All flashing around windows, at deck attachments, utility penetrations, rooflines, etc., and all kick-out flashing must be properly installed prior to application of AkroFlex System.

- Unsatisfactory conditions shall be reported to the general contractor, builder, architect, and/or owner.  Do not proceed until all unsatisfactory conditions have been corrected.

- PreparatioN

- Substrate:  Prepare the substrate to which the AkroFlex System is to be applied, ensuring that there are no foreign materials present; including, but not limited to, oil, dirt, dust, form release agents, efflorescence, paint, wax, water repellants, moisture, frost, and or extended nails.

- Surrounding Areas:  Protect surfaces near the work of this section from damage, disfiguration, and overspray.  Mask off all dissimilar materials.

- General Installation

- Refer to Intertek CCRR AkroFlex report and the appropriate manufacturer's product data sheet for additional installation requirements and recommendations.

- INSTalling joint/transition treatment [Delete if the optional water-resistive/air barrier is not used.]

- General application:  Joint/transition treatment should be applied to rough openings, sheathing joints, inside and outside corners, and tops of parapets.

[Choose one or more of the joint/transition options below.  Delete those not used]

- AkroFill with Mesh: Apply AkroFill with a trowel to the area to be treated.  The total thickness of this coat should be approximately 1/16 inch (1.6mm).  Embed AkroFlex Mesh in wet AkroFill and trowel smooth ensuring that no mesh is visible.  Sheathing joints require 4.5oz, minimum 4 inch (102 mm) wide AkroFlex Mesh.  Rough openings, inside and outside corners, window sills, and tops of parapets require 4.5oz, minimum 9.5 inch (241 mm) wide AkroFlex Mesh.  The mesh shall be lapped a minimum of 2.5 inches (64 mm) at mesh edges.  AkroFill may also be used to fill holes or surface imperfections less than 1/16 inch (1.6mm).

- AkroGuard with Fabric:  Spray, roll, or brush AkroGuard onto the area to be treated.  Embed AkroGuard Fabric in wet AkroGuard and smooth.  Apply a second coat of AkroGuard and ensuring that no AkroGuard Fabric is visible.  Sheathing joints require minimum 4 inch (102 mm) wide AkroGuard Fabric.  Rough openings, inside and outside corners, window sills, and tops of parapets require minimum 9.5 inch (241 mm) wide AkroGuard Fabric.  The fabric shall be lapped a minimum of 2.5 inches (64 mm) at fabric edges.

- Self-Adhered Flashing:  Apply self-adhered flashing to rough opening or transition per manufacturer's recommendations.  Primer may be required.  Once applied per manufacturer's recommendation, the self-adhered flashing shall be completely coated with AkroGuard.

- Installing WAter-Resistive/Air Barrier coating [Delete if the optional water-resistive/air barrier is not used.]

- Allow joint/transition treatment to dry prior to the application of AkroGuard. AkroGuard may be applied with a ¾-inch (19mm) nap roller or sprayed to form a continuous barrier across the substrate approximately 10 to 20 mils (.25 to .51mm) thick when wet.  Roller application is recommended for all rough surfaces in order to ensure a uniform application.  The application should be free of voids, pin holes, or discontinuities.  [OSB requires two separate coats approximately 10 mil (.25 mm) thick when wet.]  Allow AkroGuard to dry prior to applying second coat or installing insulation board.

- Installing Accessories

- Install accessories, including trim pieces, drip edge track, and flashing, as specified or required by local code.

- Attach accessories using corrosion resistant fasteners.

- Installing Insulation Board

- Install the appropriate starter mesh in all areas requiring wrapping prior to insulation board installation.

- Apply adhesive to backside of insulation board using a 3/8-inch x 1/2-inch x 1-1/2-inch (9.5mm x 13mm x 38mm) notched trowel.

- Apply insulation board to the substrate, long side horizontal, in a running bond pattern and tightly butting all joints.  Prevent adhesive from entering board joints.  At wall corners, board edges shall be interlocked.

- After insulation boards are firmly adhered to the substrate, fill any gaps in the insulation board layer with insulation.  Allow the adhesive to set for a minimum of 24 hours prior to rasping.

- Rasp the insulation surface to ensure a true and uniform wall is obtained.

- Installing Base coat And Mesh

- Wrapping: Complete wrapping of foam edges by applying base coat and pulling mesh tightly around the foam edge and onto the face of the insulation.  Embed mesh in the base coat while avoiding wrinkles.

- Openings and Penetrations:  Apply minimum 9.5 x 12-inch (240 x 300 mm) diagonal strips of starter mesh at corners of windows, doors, and all penetrations.  Embed mesh in the base coat while avoiding wrinkles.

- High Impact Areas:  Apply a layer of Omega Ultra Heavy Duty or Heavy Duty Mesh embedded in base coat.  Ultra Heavy Duty or Heavy Duty Mesh must butt tightly and should not overlap.  When base coat is dry, apply a layer of Omega Standard Mesh embedded in a second layer of base coat over the Heavy Duty Mesh coating.

- Standard Impact Areas:  Apply the appropriate mesh needed for the impact resistance required.  Use a double layer of mesh at all inside and outside corners and overlap a minimum of 2.5-inches (63 mm) at all mesh joints.  Embed mesh in the base coat.

- Drying:  Allow base coat to fully dry before application of primer or finish.

- Installing Primer [This section is optional and should be deleted if primer is not used.]

- Apply AkroFlex Primer with a brush, roller, or sprayer.  Avoid puddling.

- Installing Finish Coat

- General:  Apply per approved finish product data sheet.

- Verification:  Verify the desired color and texture match the approved sample and/or mock-up prior to installation.

- Field Assurance

- Proper application of the AkroFlex EIFS materials shall be the responsibility of the contractor.

- Omega Products International assumes no responsibility for application of its products or on-site inspections.

- [The contractor shall certify in writing the quality of work performed relative to the substrate system, details, installation procedures, workmanship and as to the specific products used.]

- [The EPS supplier shall certify in writing that the EPS meets Omega's specifications.]

- [The sealant contractor shall certify in writing that the sealant application is in accordance with Omega's and sealant manufacturer's requirements.]

- CLEANING

- Cleaning:  Remove any and all materials used, overspray from adjacent surfaces, and all protective masking.

- Protection

- Protection:  Protect applied material from inclement weather until dry and prevent it from freezing for a minimum of 24 hours after application and/or until dry.  Refer to product data sheet for additional requirements.

END OF SECTION 07 24 13